TEXDRAIN AF (AIR FLOW)

GAS COLLECTION/VENTING GEOCOMPOSITE

SPECIFICATION GUIDELINES

This specification is intended for use as a GENERAL GUIDELINE for developing a specification for a specific project.  It is NOT intended as a substitute for a detailed specification, which must be written to address site-specific conditions.

1.0	GENERAL

1.1	Scope

This specification covers the technical requirements for furnishing and installing the triplanar gas collection/venting geocomposite described herein.  All materials used shall meet the requirements of this specification, and all work shall be performed in accordance with the procedures and the contract drawings provided herein.

1.2	Submittals

A.	The Contractor shall furnish the following information:

- A representative sample of the gas collection geocomposite.

- Product data sheets.

- Gas collection geocomposite manufacturer's MQC Plan for documenting compliance to Sections 2.1 and 2.2 of these specifications.

- A project reference list consisting of the principal details of at least ten projects totaling at least 5 million square feet (500,000 square meters) of geocomposite.

- A gas collection geocomposite panel layout.  The predominant flow direction of the gas collection geocomposite is in the machine direction.  Accordingly, the geocomposite panels should be installed in an orientation which maximizes flow.

- Gas collection geocomposite manufacturer’s historical data for 10,000-hour creep reduction factor testing of the geonet per Section 2.1 C.

B.	Upon shipment, the Contractor shall furnish the gas collection geocomposite manufacturer's Quality Assurance/Quality Control (QA/QC) certifications to verify that the materials supplied for the project are in accordance with the requirements of this specification.

1.3	Qualifications

A.	The gas collection geocomposite manufacturer shall have successfully manufactured 5,000,000 square feet (500,000 square meters) of polyethylene geonet/geocomposite.

2.0	PRODUCTS

2.1	Materials

A.	Acceptable gas collection geocomposite products are TexDrain® AF (air flow) supplied by CETCO, 2870 Forbs Avenue, Hoffman Estates, Illinois 60192 USA (800-527-9948), or an engineer-approved equal.  For any proposed alternate product, the Contractor must furnish test results demonstrating that the proposed alternate meets all requirements of this specification (including 100-hour performance air transmissivity testing and creep reduction factor testing) for engineer approval.

B.	The geonet shall be manufactured by extruding high-density polyethylene (HDPE) to form a triaxial flow structure. The geonet shall be manufactured of polyethylene resin produced specifically for the intended application.  The natural polyethylene resin (without the carbon black) and geonet rolls shall meet the requirements in Table 1.

C.	The geonet shall have a 30-year creep reduction factor of 1.1, when tested in accordance with GRI-GC8, under a compressive load of 1,000 psf and a test duration of 10,000 hours.

D.	The geotextiles bonded to one of both sides of the geonet shall be nonwoven, needlepunched polypropylene fabrics.  The geotextile shall meet the requirements in Table 1.

E.	The gas collection geocomposite shall consist of a HDPE geonet heat bonded to either one or two layers of geotextile to create a single-sided or double-sided geocomposite, and shall meet the requirements in Table 1.  The geocomposite shall be at least 12.5 feet wide.  The geotextiles shall extend a minimum of 1 inch beyond the edges of geonet on both sides of the geocomposite roll.  The geotextile shall not be bonded to the geonet within 3 to 6 inches from the edges of the rolls.

2.2 	Manufacturer Quality Control (MQC)

A.	The gas collection geocomposite manufacturer shall provide the Contractor or other designated party with manufacturing QA/QC certifications for each shipment of material.

B.	The gas collection geocomposite (as well as the geonet and geotextile components) shall be tested by the manufacturer according to the test methods and frequencies listed in Table 1.

C.	Prior to shipment, the gas collection geocomposite manufacturer shall label each roll, identifying:

1.	Product identification information (Manufacturer’s name and address, brand product code).

- Lot number and roll number.

- Roll length, width and weight.

D.	The gas collection geocomposite shall be wound around a rigid core whose diameter is sufficient to facilitate handling.  The core is not necessarily intended to support the roll for lifting but should be sufficiently strong to prevent collapse during transit.

E.	All rolls shall be labeled and bagged in packaging that is resistant to photodegradation by ultraviolet (UV) light.

Table 1. TexDrain® AF (Airflow) Certified Properties

| Double-sided Geocomposite |
| --- |
| Property | Test Method | Test Frequency | Values |
| Air Transmissivity(1) (MD), m2/sec (load = 1,000 psf) | ASTM D4716 | 200,000 ft2 | 7 x 10-4 (i = 3) 3 x 10-4 (i = 33) |
| Peel Adhesion (MD), lbs/in | ASTM D 7005 | 100,000 ft2 | 1.0 |
| Geonet Core (2) |
| Thickness, mils | ASTM D5199 | 50,000 ft2 | 340 |
| Carbon Black Content, % | ASTM D4218 | 50,000 ft2 | 2-3 |
| Melt Flow Index, g/10 min | ASTM D1238 | Per resin lot | <1.0 |
| Density, g/cm3 | ASTM D1505 or D792 | Per resin lot | 0.94 – 0.96 |
| Geotextile Components(2) |
| Mass/Area, oz/yd2 | ASTM D5261 | 100,000 ft2 | 6 |
| Grab Tensile Strength, lbs | ASTM D4632 | 100,000 ft2 | 160 |
| Grab Elongation, % | ASTM D4632 | 100,000 ft2 | 50 |
| Trapezoidal Tear, lbs | ASTM D4533 | 100,000 ft2 | 60 |
| Puncture, lbs | ASTM D4833 | 100,000 ft2 | 85 |
| Permittivity, sec-1 | ASTM D4491 | 500,000 ft2 | 1.1 |
| AOS, US Sieve Size (max) | ASTM D4751 | 500,000 ft2 | 70 |
| UV resistance after 500 hours, % Strength Retained | ASTM D4355 | Per resin formulation | 70 |

1. Geocomposite transmissivity measured in the machine direction per ASTM D4716 with the following testing conditions: steel plate / Ottawa sand / geocomposite / 40 mil LLDPE geomembrane / steel plate, and seating period of 100 hours, with the flat side of the geocomposite facing the soft boundary as indicated with top (soil) / bottom (liner) label on the rolls.

2.  Geotextile and geonet properties listed are prior to lamination. Geocomposite properties and Geonet thickness are Minimum Average Values.  Geotextile properties are Minimum Average Roll Values, except for AOS, which is Maximum Average Roll Value.

2.3	Construction Quality Assurance (CQA)

A.	The Owner and Engineer shall provide a third-party inspector for CQA of the gas collection geocomposite installation.  The inspector shall be an individual or company who is independent from the manufacturer and installer, who shall be responsible for monitoring and documenting activities related to the CQA of the gas collection geocomposite, throughout installation.  The inspector shall have provided CQA services for the installation of the proposed or similar materials for at least 5 completed projects totaling not less than 1 million square feet (100,000 square meters).

B.	Testing of the gas collection geocomposite, as necessary to support the CQA effort, shall be performed by a third party laboratory retained by the Contractor and independent from the manufacturer and installer.  The laboratory shall have provided CQA testing of the proposed or similar materials for at least 5 completed projects totaling not less than 1 million square feet (100,000 square meters).

C.	CQA shall be provided in accordance with the project CQA Manual provided by the engineer.

3.0	EXECUTION

3.1	Shipping and Handling

A.	The gas collection geocomposite rolls shall be wrapped in a plastic cover. The gas collection geocomposite rolls shall be shipped to the job site in a manner not to damage the rolls.

3.2	Storage

A.	At the job site, geocomposite rolls shall be stored in their original, unopened packaging in a location away from construction traffic but sufficiently close to the active work area to minimize handling. The designated storage area shall be level, dry, well-drained, stable, and should protect the geocomposite from precipitation, standing water, ultraviolet radiation, chemicals, and other environmental conditions that could impact the rolls.

B.	If the integrity of the geocomposite packaging has not been affected during the shipping and unloading processes, and if the storage requirements listed herein are achieved, then the rolls may be stored on site.

3.3	Subgrade Preparation

A.	The subgrade shall be free of foreign and organic material, sharp objects, or debris of any kind, which could potentially damage the geocomposite.

3.4	Placement

A.	The geocomposite rolls shall be deployed using a spreader bar assembly attached to a loader bucket or by other methods approved by the project engineer.

B.	The Texdrain AF geonet core consists of a circular aperture side and a cuspated side.  The side with the circular apertures should be placed against the soil, while the cuspated side should be placed against the geomembrane.

C.	The geocomposite rolls shall be deployed so that, to the maximum extent possible, the machine direction of the material aligns with the direction of the steepest slope.

C.	On slopes the geocomposite shall be secured in the anchor trench as shown on the project drawings and then rolled down the slope. Rolls should be deployed in such a manner as to continually keep the geocomposite panel in sufficient tension to reduce folds and wrinkles.

D.	In the presence of high wind, sandbags shall be placed on leading edges of the panels to prevent wind uplift.

E.	If there are any penetrations (such as outlet pipes or monitoring wells) while deploying the drainage geocomposite, the geocomposite should be cut to fit around the penetration.  Care must be taken to ensure there is no gap between the penetration and the geocomposite, to prevent soil particles from migrating into the geonet core.  If the material is being cut in place, special care must be taken to protect other geosynthetic materials from damage.

G.	Care shall be taken not to entrap stones, soil, or excessive dust that could damage the geocomposite, or generate clogging of drains or filters.

3.5	Seams and Overlaps

A.	When connecting the rolls side-to-side, the geonet shall be overlapped 2 to 3 inches and tied together.  The geonet shall be tied together every 5 feet along the length of the panel.  The geonet in the anchor trench at the top of the slope shall be tied at 6- to 12-inch intervals.

B.	When connecting geocomposite rolls end-to-end, the geonet shall be overlapped a minimum of 12 inches, shingled down in the direction of the slope, with the geonet portion of the top geocomposite overlapping the geonet portion of the bottom geocomposite.  Geonet shall be tied every 12 inches across the roll width.  No horizontal seams shall be allowed on side slopes greater than 4:1, unless approved by the design or CQC/CQA engineer.

C.	The geonet shall be tied with plastic fasteners (e.g. cable ties).  Tying devices shall be white or yellow for easy inspection.  Metallic devices are not allowed.

D.	The bottom geotextiles shall be overlapped, or at the discretion of the engineer, sewn together.

E.	The top geotextiles shall be overlapped and continuously sewn or thermally bonded, per the project specifications.  If thermal bonding is to be used, care must be taken to avoid burn through of the geotextile.

3.6 	Repairs

A.	Prior to covering, all panels shall be inspected for damage.

B.	Any small holes or tears in the top geotextile shall be patched with a 8” x 8” geotextile patch.  The patch can be adhered using a spray adhesive (such as 3M Super 77).  If the damaged area of the geotextile is greater than the standard patch size, then a larger patch is recommended.  If the geotextile is damaged beyond 50 percent of the roll width, a full-width geotextile cap-strip shall be used.

C.	Damaged areas on the geonet core shall be patched by placing a geonet or geocomposite patch extending 12 inches beyond the edges of the damaged area.  The patch shall be secured to the original geonet with ties every 6 inches.  If the damage on the geonet portion of the deployed geocomposite is more than 50 percent of the roll width, the entire section shall be cut out, and the two geonet sections shall be joined together end-to-end, as discussed in 3.5.

3.7 	Covering

A.	The gas collection geocomposite shall be covered after deployment and approval by the responsible party.  Geocomposite shall be covered within 14 days.

B.	The covering operation shall not damage the gas collection geocomposite. The cover soil material shall be free of foreign and organic material, sharp objects, or debris of any kind, which could potentially damage the geocomposite.  Cover soil shall be placed on the geocomposite using wide track equipment, starting at the bottom of the slope proceeding upwards.

C.	No construction equipment shall operate directly on the geocomposite. The use of lightweight machinery with low ground pressure (i.e., ATVs) is allowed.